## Slide 1: Constitutive Models for viscoelasticity
Presented by:
Ayush Tripathi
Under the guidance of
Dr Prakhar Gupta
Department of Mechanical & Aerospace Engineering

## Slide 2: Index
Framework
Internal variable model
Continuum mechanics model
Rheological model
Strain energy density functions
Micro macro model
Statistical mechanics framework
Honeywell project
Roadblocks
course of action

## Slide 3: Introduction
Development of constitutive models based on two approaches
  Continuum Mechanics framework
    Internal variable
    Thermodynamic variable
  Statistical Mechanics framework
    Micro-mechanism

## Slide 4: Continuum mechanics framework
Also referred as phenomenological models.
Such models assume that the hyperelastic properties can be described by means of a strain energy density function that involves either strain invariants or principal stretches.
All hyperelastic material models are based on a strain energy function that determines how much energy is stored in the material as a function of the applied deformation
Since the energy must be independent of rigid body rotations, the strain energy function is often written in terms of its invariants
Lack microstructural justification

## Slide 5: Statistical mechanics framework
Directly link the macroscopic behavior of the materials to their microstructure.
The parameters of polymer physics and chemistry, such as the cross-linking density, the molecular weight of the monomers, the chain extensibility, the polymerisation degree and the amount of entanglements of polymer chains, reflect the microstructure of the material
Micro-mechanical based hyperelastic models
Preserve the affinity of network deformation induced by the macroscopic deformation
Affine network models fail to fully capture the entanglement effect of polymer chains, hence cannot represent the real molecular structure of the elastomers.

## Slide 6: Constitutive models with Internal variables
Current state of thermoelastic material
  F and θ
  Measurable and controllable (External variable)
Material involving dissipation
  Internal variable
    Describes aspects of the internal structure of a material
    History variable for dissipative materials
  Thermodynamic state variable ζ
Current state of dissipative material : F, θ, ζ

## Slide 7: Constitutive models with Internal variables
Current thermodynamic state: fictitious state of thermodynamic equilibrium described by their current value and not by their past history
phenomenological variable constructed mathematically(Thermal, chemical, mechanical)
Describe structural property within a macroscopic framework
  Dashpot displacement in viscoelastic models
  Damage, inelastic strains, dislocation densities
The existence of non-equilibrium states that evolve with time is an essential feature of inelastic materials
A viscoelastic behaviour of a material is characterised by hysteresis

## Slide 8: Isothermal framework
Hemholtz free energy function defines the thermodynamic state by
  Deformation Gradient (F)
  Internal history variable specified for a particular problem
Number of variables depend on theory and boundary condition

## Slide 9: Constraints on constitutive law
it is essential to make sure that the stress-strain law satisfies two conditions:
(i) It must obey the laws of thermodynamics.
(ii) It must satisfy the condition of objectivity, or material frame indifference.
Thermodynamic restrictions: The laws of thermodynamics impose two restrictions on stress-strain laws:
The first law requires that the work done by stresses must either be stored as recoverable internal energy in the solid, or be dissipated as heat (or a combination of both).
The second law requires that if a sample of the material is subjected to a cycle of deformation that starts and ends with an identical strain and internal energy (at constant temperature, or without heat exchange with the surroundings) the total work done must be positive or zero.

## Slide 10: Constraints on constitutive law
Local entropy production must always be greater than zero
Work conjugate pair; rate of internal mechanical work per unit volume (stress power)
Rate of change of internal energy
For purely mechanical theory

## Slide 11: Internal variable model
Must hold for all times at every point of the continuum body
Conjugate to
Tensor variables F and are associated with thermodynamics forces P and
If is not needed to characterize thermodynamic state of the system, then the material is perfectly elastic
Gradient of free energy wrt to internal variable
Splitting the terms
Notes: 281

## Slide 12: Kinetic Relation
Describes the evolution of the internal variable and associated dissipation mechanism
Required to describe how an irreversible process evolves
Thermodynamic admissibility is the only restriction
Rate at which the internal variables tend towards equilibrium
Tensor valued function with 1+m variables
Every system tends to thermodynamic equilibrium
  Observable and internal variable reach equilibrium under prescribed stress and strain
  Remain constant at all points if the system with time
For an elastic continuum, every state is in equilibrium

## Slide 13: Viscoelastic material at large strains
Process involving relaxation and creep
  Non equilibrium thermodynamics
  Thermoplastic elastomers
Thermodynamic state is characterized by internal variables
External variables not suitable for finite element realization
3D viscoelastic model for finite strains and small perturbations away from equilibrium
Not restricted to isotropy

## Slide 14: Viscoelastic material at large strains
Decoupled representation of Helmholtz free energy function
  Dialational
  Isochoric
Change of free energy within an isothermal framework given by
Normalization condition
Equilibrium state
Configurational

## Slide 15: Viscoelastic material at large strains
Third term
  Represents configurational free energy
  Characterizes non equilibrium state(behaviour of relaxation and creep)
   function of strain like internal variables (inelastic,) akin to C

## Slide 16: Decoupled volumetric-isochoric State
Second Piola-Kirchoff
Additive decomposition
Where,
    Q represents non-equilibrium stresses in the sense of non-equilibrium thermodynamics
    P is the projection tensor

## Slide 17: Viscoelastic material at large strains
Equilibrium
Non-Equilibrium
Fictitious Non Equilibrium Stress
Q are the conjugate to
The conditions restrict configurational free energy
As t 
Q represents distance from equilibrium
Dissipation at equilibrium is zero
At thermodynamic equilibrium the material responds perfectly elastic

## Slide 18: Rheological models
= Relaxation Time of the subnetwork
Solid behaviour is modelled by set of springs responding linearly according to hooke’s law
The stiffness of the free spring and springs of α-maxwell element are determined by young’s moduli
Flow behaviour is modelled by viscous fluid like dashpot
  Total Stress applied
  Total linear strain due to strain
  inelastic strain(internal variable)
  Strain rate
  Viscosity
  -
  Non equilibrium stress(internal variable) at each dashpot

## Slide 19: Rheological models
The Mechanical device is assumed to have unit area and unit length
  Stress and strain interpreted as force and extension
  Total stress applied
  @ equilibrium
  Stress in the spring of α-maxwell element
  Stress acting on each dashpot
  Differentiating, we get

## Slide 20: Thermodynamic Admissibility
 stress on each dashpot
 strain rate on each dashpot
Always non-negative
Condition for Thermodynamic admissibility of non-equilibrium stress

## Slide 21: Stress Decomposition
Defining Strain energies
  Where, the quadratic forms
  Normalization condition

## Slide 22: Stress Decomposition
 Energy stored elastically in springs
Viscoelastic contribution to strain energy and is related to relaxation(retardation) process with relaxation time
Differentiating () wrt total strain () gives the total stress () applied
Non-Linear Stress
Linear Stress
The internal dissipation becomes

## Slide 23: Evolution Equation
Necessary to specify complementary equations of evolution
  Describes evolution of a viscoelastic process
  Local entropy production inequality is satisfied
Law needs to govern internal variable
  -- Isochoric non-equilibrium stress
Evolution equation needs to have physical basis
Should be suitable for time integration algorithm
Good approximation to the observed physical behaviour for large strain

## Slide 24: Evolution Equation
we start from stress free configuration @ t=0
Isochoric second PK corresponding to strain energy
  Depends only on external variable C
  Responsible for relaxation(retardation) process with relaxation(retardation) time
  constitutive equation for fictious second PK
  Both Q and S contribute to the isochoric response

## Slide 25: Solution to linear evolution equation
Solution to the evolution equation valid for semi-open interval
Instantaneous response is given by
Evolution of internal variable is governed by strain energy density function

## Slide 26: Solution to linear evolution equation
If the viscoelastic medium such as thermoplastic elastomer is composed of identical polymer chains, we replace
The expression becomes
Are given non-dimensional strain energy factors associated with (Simo and Govindjee)

## Slide 27: Time integration algorithm
Cauchy’s equation of motion
We need an update algorithm to obtain total stress
Update procedure recognized in reference configuration
  Numerical integration of convolution integral
Algorithmic update of the second Piola Kirchhoff stress S
Time discretization of the closed time interval

## Slide 28: Time integration algorithm
For a time sub interval
Assuming that upto a certain time , the stress Sn , satisfies the equilibrium equation and displacement field Un
    Fn = I + Grad Un Jn= det Fn
    Cn= FnT Fn C n= Jn-2/3 Cn
    Sn Determined previously
Are specified uniquely by a given motion Xn at time
Strain driven type of numerical procedure

## Slide 29: Time integration algorithm
We advance the procedure to time
  Update all relevant quantities
  Make an initial guess Xn+1  trial solution
  Update all prescribed loads
The new motion Xn+1 at time tn+1 is corrected iteratively until all balance principles are satisfied
To check equilibrium at tn+1 all the tensor variables are updated
    Fn+1 = I + Grad Un+1 Jn+1= det Fn+1
    Cn+1= Fn+1T Fn+1 C n+1= Jn+1-2/3 Cn+1

## Slide 30: Time integration algorithm
Sn+1 at tn+1 is determined uniquely via associated constitutive relation
All strain measures are known at tn+1

## Slide 31: Time integration algorithm
For using the approach followed by (Simo 1987), which bypasses the need for incremental objectivity (frame indifference) during superimposed rigid body motion
Splitting the convolution integral

## Slide 32: Time integration algorithm
To simplify we substitute
takes values and
Using second order accurate mid point rule on the third term

## Slide 33: Time integration algorithm
Rearranging and substituting we get,
where
Dimensionless parameter
History term determined by Q and S from previous iteration.

## Slide 34: Micro mechanical based model
Elastomers consist of polymer networks formed by the cross-linking of highly mobile and flexible polymer chains
typically characterized by their high compliance and capability of sustaining large deformation
Non linear stress behaviour
  Sustain strain upto few hundred percent (Hyperelasticity)
  Rate dependent behaviour(viscoelasticity)
Decompose stress
  Elastic + Inelastic

## Slide 35: Micro mechanical based model
Phenomenological model
  Properties of material defined using strain energy density function
  Strain invariants and principal stretches
Models sufficient to describe empirical relationship between stress and strain
  Lack microstructural justification

## Slide 36: Micro mechanism model
Directly link macroscopic behaviour to their microstructure
Considering parameters of polymer physics and chemistry
  Cross-linking density
  Molecular weight of monomers
  Chain extensibilty
  Polymerization degree
  Amount of entanglement of polymer chains
Gaussian: chain length <<< extension limit
Non-gaussian: chain length approaches maximum extension
Fail to capture entanglement effects of chain

## Slide 37: Multiplicative decomposition of deformation gradient
Stress or strain like internal variable
Similar to finite deformation plasticity
Multiplicative decomposition of deformation gradient
Microstructure details are not reflected by the material parameter
Capable of qualitatively predicting
  Time dependent inelastic deformation
  Stress response of elastomers
Distinguish between them by
  Numerical modelling on macroscopic viscoelastic behaviour
  Fitting to experimental behaviour
Lack underlying physical mechanism of viscoelasticity

## Slide 38: Polymer Dynamics: Tube model
Cross Linked with chains at C and D
Entanglement with chains at C and D
Topological constraint: Polymer chain is confined in a tube like region
Primitive chain: Axis of tube confining chain C-D

## Slide 39: Polymer Dynamics: Tube model
For short time scales
  motion of polymer chain can be considered as wriggling around its primitive chain
Wriggling represented by
  Dia of tube
  Contour length of primitive chain
  Motion forgotten once parameters are defined
For long time scales
  Polymer chain reptates along the tube
  Destroying and creating ends of the tube

## Slide 40: Polymer Dynamics: Tube model
Under deformation
  Ground network sustains elastic stress
  Inelastic stress is generated by reptation
  Dia of tube changes significantly
  Affects the reptation ability and hence relaxation process
Needs to be developed statistically
  All parameters have microscopic foundation
  Obtained by fitting experimental data/ simulation
cannot be used to capture the energy dissipation during finite deformation

## Slide 41: Micro macro constitutive model
Micro macro constitutive model
  Combines continuum mechanics and statistical mechanics
  Incorporates non-linear viscosity into state of art continuum mechanics
  Adopts thermodynamic evolution model
  adopts most of the hyperelastic constitutive equations
  Captures the relaxation and non-linear viscosity of polymer chains under large deformations
  Insights into tailoring the microstructure to application

## Slide 42: Continuum mechanics Framework
Elastic ground network
Subnetwork of different types of polymer chains
Each subnetwork represents a type of polymer chains with similar diffusion behaviour
Subnetworks B1 –Bm relax with time and dissipate energy
Deformation gradient is
Since deformation acts on all the polymer network

## Slide 43: Continuum mechanics Framework
For each subnetwork, F can be decomposed into
  Elastic Component
  Inelastic component
 Deformation gradient of the spring
 Deformation gradient of the damper in the subnetwork

## Slide 44: Continuum mechanics Framework
& Helmholtz free energy densities of the spring in ground and sub network respectively
Total free energy density of the elastomer
Cauchy stress tensor is given by

## Slide 45: Continuum mechanics Framework
Where,
First piola Kirchoff stress tensor is given by

## Slide 46: Thermodynamic requirement
free energy of a material system must never increase under isothermal conditions.
  internal variables of the time-dependent polymer networks must fulfil the entropy inequality
Even when the system is in a non-equilibrium state

## Slide 47: Internal variable evolution equation
We know that
Material time derivative of internal variable,
Where,
Load is applied simultaneously to all networks simultaneously
Relaxation of different subnetwork is independent of each other
Notes: Coleman and gurtin

## Slide 48: Thermodynamic admissibility
A sufficient condition for fulfilling the inequality is that the internal variable satisfy the thermodynamic evolution equation
Notes: From(using) kinetic relation slide 7, time

## Slide 49: Rivlin-Mooney
Linear dependence on first and second invariance
applicable for small strains only
Cannot capture strain hardening or softening
Lack of frequency dependence
Parameters lack physical basis

## Slide 50: Neo-Hookean Model
µ and k are material parameters
For small strain, they are shear and bulk modulus respectively
µ =NkT; where N is the number of polymer chains per unit volume, k is the Boltzmann constant, and T is temperature.
Limited compressibility
Does not account for variation in Material parameters with strain rate
Not suitable for finite deformation

## Slide 51: Ogden
Stretch based
Modified principle stretches associated with volume changing deformations
Choices of independent variable complicate the mathematical analysis associated with it
Versatile (compressible and incompressible material)
Highly parameterisable
Suitable for finite deformation; high strain range
Limited capture of nonlinearities
Parameters does not have physical basis
Can be reduced to Rivlin-Mooney

## Slide 52: Gent
Singularity when the first invariant of the left Cauchy-Green deformation tensor reaches a limiting value
Finite stretchability
Accounts for chain extensibility

## Slide 53: Stress-strain relation

## Slide 54: Non-linear viscosity of free chains
The viscosity of subnetwork Bn must be constitutively prescribed to obtain inelastic deformation
viscosity of a polymer network can be expressed in terms of the shear relaxation modulus Gn
Relaxation of elastomers originate from the polymer chains

## Slide 55
For short time scale(t<te)
  Diffusion of the polymer chain can be represented as Brownian motion
For (t=te)
  Brownian motion restricted by topological constraint (tube region)
For (t>te)
  Due to restriction on the tube, the polymer chain starts to reptate and disengages from the original tube
Assuming smooth transition from rouse behaviour to reptation behaviour, G in terms of polymer structure parameter
Non-linear viscosity of free chains

## Slide 56: Non-linear viscosity of free chains
During reptation
  Parts of chain disengage from tube
  Only the parts still confined in the tube contribute to the stress
  The relaxation modulus Gn is proportional to the fraction of the chain still confined in the tube at time t (i.e. Gn = )
  We define (s) as the contour position of the segment on the primitive chain and as the probability that the primitive chain moves while its ends have not reached the segment (s) of the original tube

## Slide 57: Non-linear viscosity of free chains
must satisfy the one dimensional diffusion equation
  Dc is the diffusion coefficient of the polymer chain
  When ξ = s, segment s disengages from the original tube and
  Similarly when ξ = s-L, where L is contour length of the primitive chain at time t
  The solution using the boundary conditions

## Slide 58: Non-linear viscosity of free chains
Where is the disengagement time of the free chain
  Time needed for complete disengagement of the polymer chain from the tube it is confined or finish the relaxation process
Fraction of chain confined in the tube at time (t)
Combining, we get
where
 Tube diameter
monomer friction coefficient
Polymerisation degree of network
bo effective bond length between monomers

## Slide 59: Non-linear viscosity of free chains
of the tube and primitive chain length are assumed to be unchanged under deformation (Doi and Edwards 1986)
  Which yields a constant
  Works well for small deformations
To capture the nonlinear viscosity under finite deformation
  The primitive chain length L must change with macroscopic deformation
  Average over all possible initial tangent vectors u0 is formulated as
  The mean diameter (an)also changes with deformation
    Linked to mean square end-to-end distance of the primitive chain
  Assumptions have been verified using molecular dynamics simulation

## Slide 60: Non-linear viscosity of free chains
In this model, the disengagement time in the equation of viscosity varies with macroscopic deformation
Leading to non-linearity of viscosity
Here, the mean square end-to-end distance of the primitive chain is calculated as
f0(R) is the statistical distribution function on end-to-end vector R of the primitive chain in reference state

## Slide 61: Non-linear viscosity of free chains
Assumed that the primitive chain in the current state is deformed in the same way as the microscopic deformation therefore,
  a0= diameter in the primitive chain
  = mean square end-to-end vector of the primitive chain in the reference state
Substituting in the equation for non-linear viscosity
Viscosity in reference state
Dimensionless parameter

## Slide 62: Numerical simulations
Helmholtz free energy density functions must be specified first
Governed by elastic ground network of the polymer
  Should be able to capture elastic response of the elastomer
  Material parameters can be obtained by fitting them to quasi-static experiments
The material parameters of can be be determined by fitting them to loading-unloading experiments conducted at different strain rates
Considering homogenous isochoric deformation

## Slide 63: Honeywell project: Gel preparation
Prepared 36 Gel samples replicating bird material
Cut 75 mm dia plastic tubes with 180 mm length
  To be used as a mould
  Prepare wheat dough with a dry consistency for sealing
  Spread the dough 10mm thick on a rigid tray
  Stick the pipes in dough to obtain a proper seal
  Spray silicon nitride to prevent gel from sticking to the pipe
Prepared gel with 1000 kg/m3 density
  10 % Gelatine (w/w)% in water
  Mix thoroughly and let it sit for 1-2 hours
  Heat the beaker in water bath maintaining 55 until homogenous solution is obtained
  Pour the solution in the pipes till 155mm height from dough surface
  Refrigerate at 5-15 for 18 to 36 hours

## Slide 64: Setup
Mould removal
  Dip the cast in warm water briefly
  Use a long thin metal wire to slowly debond the curved surface of the pipe
  Gently apply pressure from free end to obtain the required gel cylinder
Helped in the initial setup of the
  Strain gauge
  Gas gun
  Barrel
  Momentum trap